## Slide 1: Development of an Automated Strategy to Calibrate Crystal Plasticity Subroutines for ABAQUS, Using Machine Learning Approaches, and Neural Networks
Orkun Karagüllü
Examiner : Prof. Dr. Ing. Münstermann, Dr. Ing Michael Dölz
Supervisor: Henrich Manuel, M.Sc.

## Slide 2: Motivation and Aim
Conventional crystal plasticity (CP) calibration routines are user dependent, and time consuming.
Decreasing the user dependency via using machine learning algorithms.
Automate the process for a faster and parallel calibration routines.
A robust and flexible model that can be used in different phases.
Force Displacement Curve

## Slide 3: Nanoindentation Test
Nanoindentation results of bainite and ferrite phases have been obtained from the X65 Pipeline (PL) and DP780 Dual-Phase (DP) steels.
Piezoelectric Sensor

## Slide 4: Crystal Plasticity Model
Parameter | Min. | Max.
, MPa | 43 | 354
, MPa | 148 | 837
 | 1 | 5
, MPa | 180 | 1518
Parameter | Min. | Max.
 | 43 | 354
 | 148 | 837
 | 1 | 5
 | 180 | 1518
Slip rate
Initial critical resolved shear stress
Back stress evolution law
Resolved shear stress
Critical resolved shear stress

## Slide 5: Artificial Intelligence (AI) Model
Simulation Output
(Force-Displacement Data)
AI Simulation Input
(CP Parameters + Displacement)
AI Conducted Simulation Output
(Force Data)
Training Data
Experimental (True) Data
Best 25 AI Conducted Simulations
Verification
Comparison
Simulation Input
(CP Parameters)

## Slide 6: AI Model
Automation
Script
Latin Hypercube Sampling

## Slide 7: AI Model
DP Steel
PL Steel

## Slide 8: AI Model
Simulation Output
(Force-Displacement Data)
AI Simulation Input
(CP Parameters + Displacement)
AI Conducted Simulation Output
(Force Data)
Training Data
Experimental (True) Data
Best 25 AI Conducted Simulations
Verification
Comparison
Simulation Input
(CP Parameters)

## Slide 9: Best AI Conducted Simulation for DP Steel
AI model able to optimize CP parameters of both phases.
The flexibility criteria is achieved.
PL Steel
DP Steel

## Slide 10: Response Surface Model
Gloabal Sensitivity Analyze
Statistical Method to Generate Samples
Abaqus CPFEM Model
Performing Batch of Simulations
Latin Hypercube Sampling
Morris Method
Root Mean Square Error
Error Function
Polynominal Fitting
Creating Response Surface
Particle Swarm Optimization
Optimizing Simulation Parameters
PSO

## Slide 11: Morris Sensitivity Analysis
One step at a time method.
Measures elementary effect of each parameter on the output.
, MPa | , MPa | a | , MPa
43 | 745 | 1 | 1518
43 | 561 | 1 | 1518
250.3 | 561 | 1 | 1518
250.3 | 561 | 3.7 | 1518
 |  | a | 
43 | 745 | 1 | 1518
43 | 561 | 1 | 1518
250.3 | 561 | 1 | 1518
250.3 | 561 | 3.7 | 1518

## Slide 12: RS for DP Steel
Exploration
1. Exploitation
2. Exploitation

## Slide 13: RS for PL Steel
Exploration
1. Exploitation
2. Exploitation

## Slide 14: Error Function

## Slide 15: Weighted Error
Weighted Error = WE
Area Under the Curve = AUC
Difference in Maximum Load = DML
Source: LI, H., L. GUTIERREZ, H. TODA, O. KUWAZURU, W. LIU, Y. HANGAI, M. KOBAYASHI und R. BATRES. Identification of
material properties using nanoindentation and surrogate modeling .

## Slide 16: RS for DP Steel
Exploration
2. Exploitation
1. Exploitation

## Slide 17: Conclusion
AI Results
RS Results
User dependency
Computational cost
Required time
Flexibility
Accuracy

## Slide 18: Calibration of CP Parameters
Nanoindentation test
  Force – Displacement Curve
  Pile Up
CPFEM
Validation on Hysterisis Loop

## Slide 19: Intelligent Calibration of CP-Parameters
Experimental vs. simulation pileups:
Measured with Atomic Force Microscopy
Extracted coordinates from penetrated surface

## Slide 20
Simulation Output
(Force-Displacement Data
+Pileup Data)
AI Simulation Input
(CP Parameters + Displacement + Pileup)
AI Conducted Simulation Output
(Force Data)
Training Data
Experimental (real) Data
Best 25 AI Conducted Simulations
Simulation Input
(CP Parameters)
Intelligent Calibration of CP-Parameters